Feeds and Speeds
Feed rate (cutting speed) and Power (percentage of maximum laser power) typically need to be tuned for each material. Even among the same material, there is often variation, so the numbers presented here are just starting points. Some adjustment of these settings are usually necessary to achieve the results you’re looking for. Because of this, it is advised to cut some test samples before cutting a large project to ensure that you’re getting good results. Note that in order to extend the life of the laser, it is advised to never exceed 50% power.
## Material: Plywood
	Cut		Engrave/Score
Thickness	Power (%)	Speed (mm/s)	Power(%)	Speed(mm/s)
3mm (1/8 in)	50	15-20	15	200
5mm (3/16 in)	50	10-13	15	200

## Material: Acrylic
	Cut		Engrave/Score
Thickness	Power (%)	Speed (mm/s)	Power(%)	Speed(mm/s)
3mm (1/8 in)	50	20-25	15	200
5mm (3/16 in)	50	7-10	15	200

## Material: High density fiber board (Hardboard or HDF)
	Cut		Engrave/Score
Thickness	Power (%)	Speed (mm/s)	Power(%)	Speed(mm/s)
3mm (1/8 in)	50	15-20	15	200
5mm (3/16 in)	50	10-13	15	200